## Slide 1
Optical mode size influences the high frequency performance
3D Optical investigation of Mode Volume

## Slide 2
1.25 um radius
2021

## Slide 3
Lithographic defined VCSELs
Higher performance due to elimination of strain induced by the oxide and better thermal performance
Current confinement by proton implantation?
Not clear why thermal behavior is that better.

## Slide 4
TJ VCSELs combine all those advantages in one stroke !
Elimination of strain induced by the oxide, the ultimate reason for reliability issues

## Slide 5
TJ VCSELs combine all those advantages in one stroke !
Elimination of strain induced by the oxide, the ultimate reason for reliability issues
Precisely defined optical and electrical confinement

## Slide 6
TJ VCSELs combine all those advantages in one stroke !
Elimination of strain induced by the oxide, the ultimate reason for reliability issues
Precisely defined optical and electrical confinement
Better heat behavior

## Slide 7
TJ VCSELs combine all those advantages in one stroke !
Elimination of strain induced by the oxide, the ultimate reason for reliability issues
Precisely defined optical and electrical confinement
Better heat behavior
Smaller Mode volume

## Slide 8
Optical mode size in Oxide/Relief confined VCSELS
Standard Oxide VCSEL
Contact Ring

## Slide 9
Optical mode size in Oxide/Relief confined VCSELS
Standard Oxide VCSEL
TJ VCSEL
Contact Ring
10nm TJ Relief

## Slide 10
Optical mode size in Oxide/Relief confined VCSELS
Standard Oxide VCSEL
TJ VCSEL
Contact Ring
10nm TJ Relief
3 l cavity
3 TJ VCSEL

## Slide 11
Contact Ring
Threshold Difference = (1-G0/G1)x100
G1
G0
Standard Oxide VCSEL

## Slide 12
10nm TJ Relief
TJ VCSEL

## Slide 13
10nm TJ Relief
1.25 um exp.
Minimum at 0.75 um OXIDE radius
Close to Berlin results

## Slide 14
10nm TJ Relief
Factor 5 !
Minimum at 0.75 um OXIDE radius
Minimum at 0.40 um for TJ radius

## Slide 15
3 l cavity
3 TJ VCSEL

## Slide 16
Reason for Modal Volume difference:
Oxide (dashed lines) provides a much lower confinement.

## Slide 17
Reason for Modal Volume difference:
Oxide (dashed lines) provides a much lower confinement.

## Slide 18
Single mode operation
In summary
Oxide
TJ
Threshold
Mode Volume
20nm TJ relief, 0.5um radius
Gth=2000/cm

## Slide 19
Effect of TJ-relief height: small volume
Fmax x 2
Fmax x 3, BUT Gth x 4

## Slide 20
Fmax x 1.5
Effect of TJ-relief height: standard volumes
Better SM
performance
Not too bad
threshold penalty

## Slide 21
Relief scattering loss investigation
1
2
3
1
2
3
Size
TE comp.
TM comp.
Total Reflection at
air interface
Scattering
losses
Notes: EigTOT.fig, da aprire con Matlab2015

## Slide 22
Relief scattering loss investigation
1

## Slide 23
Relief scattering loss investigation
2

## Slide 24
Relief scattering loss investigation
3

## Slide 25
Relief scattering loss investigation
1
2
3
1
2
3
Size
Metal Ring
Air interface
QW section
Notes: Gth_th6.fig da TJTH-6-1-RED_0_Diel0_Loss-10_Mir5_IK1
PzFINAL

## Slide 26
Effect of thermal lensing
Standard Oxide VCSEL
Lithographic VCSEL 20nm Relief
Delta_Tmax= 40 and 100
Notes: plotGaAs
MainGaAsOxTEMP MainGaAsMETtjth6TEMP
fi_add= 'TempOxREFpp-0-RED_0_Diel0_Loss-10_Mir5_IK1’ fi_add= 'TempTJTH-6-1-RED_0_Diel0_Loss-10_Mir5_IK1'

## Slide 27
Dynamics: preliminary results Martino D’Alessandro

## Slide 28
Dynamics: preliminary results Martino D’Alessandro
Period 0.1 ns (10GHz)

## Slide 29
Dynamics: preliminary results Martino D’Alessandro
Period 0.1 ns (10GHz)